Technical Data Sheet of SOFA IV140

Description:Vegetable Base

Appearance:Liquid

Applications:FAC producted through hydrolysis, distillation and other processes based on soyabean oil. Suitable for dimmer acid, alkyd resin, surfactant, synthetic detergent and so on.

Packing:180Kgs net/PE Drum or 20MT net/Flexitank

| Item | Test Method | Qualified Value |
| --- | --- | --- |
| Appearance | Visual | Liquid 25℃ Conform |
| Colour(Fe-Co) | GB/T1722 | 3 Max |
| Acid Value(mgKOH/g) | GB/T9104.3 | 195-207 |
| Iodine Value(gl2/100g) | GB/T9104.1 | 140 Min |
| Saponification Value(mgKOH/g) | GB/T9104.2 | 196-208 |
| Solidifying Point(℃) | GB/T9104.5 | 20 Max |
| Moisture(%) | GB/T9104.6 | 0.3 Max |

- Email: a1824203@163.com    Whatsapp:+8618242038428