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Description:Vegetable Base
Appearance:Liquid
Applications:FAC producted through hydrolysis, distillation and other processes based on soyabean oil. Suitable for dimmer acid, alkyd resin, surfactant, synthetic detergent and so on.
Packing:180Kgs net/PE Drum or 20MT net/Flexitank
	Item
	Test Method
	Qualified Value

	Appearance
	Visual
	Liquid 25℃ Conform

	Colour(Fe-Co)
	GB/T1722
	3 Max

	Acid Value(mgKOH/g)
	GB/T9104.3
	195-207

	Iodine Value(gl2/100g)
	GB/T9104.1
	140 Min

	Saponification Value(mgKOH/g)
	GB/T9104.2
	196-208

	Solidifying Point(℃)
	GB/T9104.5
	20 Max

	Moisture(%)
	GB/T9104.6
	0.3 Max
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